SLIP RESISTANCE TEST REPORT

Client: Tile Warehouse	Tested By: Kevin Stackhouse

Client's Reference: BLNGF40	        Date: 19TH July 2005

DESCRIPTION OF SAMPLE

Manufacturer: Granite	Material Type: Granite Tile

Common Name: Black Nero Flamed	 Surface Type: Flamed

Specimen Size: 400mm x 400mm	           Colour: Black

# No. of Specimens Tested: Five                                Surface Coating: Nil

METHOD

Tests were carried out in accordance with AS/NZS 3661.1 : 1993 Slip Resistance of Pedestrian Surfaces, Part 1- Requirements, Appendix A "Method for the Measurement of the Coefficient of friction of Wet Surfaces".

Type of Test: Unfixed	Location of Test: Safety Step Workshop

Air Temperature: 17(C

RESULTS

| Specimen No. | Dilution Ratio | Dwell Time | Mean Coefficient of Friction |
| --- | --- | --- | --- |
| one |  |  | 0.57 |
| two |  |  | 0.59 |
| three |  |  | 0.61 |
| four |  |  | 0.61 |
| five |  |  | 0.59 |

SAMPLE MEAN COEFFICIENT OF FRICTION:   0.59

REQUIREMENTS

Horizontal Surfaces: When tested in accordance with the method set out in Appendix A, the pedestrian surface shall have a mean coefficient of friction of not less than 0.40

and no specimen in that sample shall be less than 0.35.

COMMENTS: